## Slide 1: NCAT Pavement Test Track
Preservation Research Update

## Slide 3: Background
Crack/fog seal
Chip/slurry/micro
Thin overlay
Thick overlay
Shallow mill/inlay or hot recycle + overlay
Deep mill/inlay or cold recycle + overlay(s)
Reclamation + overlay(s)
Select for
Lowest Life
Cycle Cost

## Slide 4: Preservation Group (PG) Experiment
Need to quantify the benefits of preservation
Good materials, designs, placement quality
Designs verified with actual onsite materials
All rates calibrated before and verified as placed
MAP-21 (cracking, rutting, roughness) focus
Many other non MAP-21 performance measures
Benefits as function of pretreatment condition
Agency decision process implementation.

## Slide 5: Preservation Options Studied
Emulsion surface treatments
  Fog seals with, without rejuvenators
  Chip seals with, without rejuvenators (scrubs), fibers
  Micro surface with, without HiMA, fibers and double
  Micro surface as Cape seals on chips, scrubs.
Plant produced thinlays
  4.75 DGA (virgin, 50% RAP, 5% RAS, 11% RAP + 3% RAS)
  DGA Thinlays over 100% RAP cold recycle (CCPR, CIR)
  DGA Thinlays as “HMA Capes” on chips and scrubs
  Open graded friction course (OGFC) surfaces (tack study)

## Slide 6: Lee Road 159 Low Traffic Preservation
70k ESALs
880k ESALs
Notes: As of April 2016

## Slide 7: US-280 High Traffic Preservation
5.6M Vehicles, 1.6M ESALs
Notes: As of April 2016

## Slide 8: Cold Climate Sections

## Slide 9: Cold Climate Sections
710 ADT with 8% Heavy Commercial
16,500 ADT with 3% Heavy Commercial

## Slide 10: Similar Findings
SINGLE MICRO SURFACE
SINGLE MICRO SURFACE + CRACK SEALING

## Slide 11: Benefits = f(Pretreatment Condition)
MAP-21 Cracking
Green = “Good” (< 5%)
Yellow = “Fair” (5% ≤ 20%)
Red = “Poor” (> 20%)
“Fair”
Condition
Improving
Benefit at
End of
Year 5
“Fair” Life Extending Benefit
Notes: As of April 2016

## Slide 12: Benefits = f(Pretreatment Condition)
MAP-21 Cracking
Green = “Good” (< 5%)
Yellow = “Fair” (5% ≤ 20%)
Red = “Poor” (> 20%)
Notes: As of April 2016

## Slide 13: Benefits = f(Pretreatment Condition)
MAP-21 Cracking
Green = “Good” (< 5%)
Yellow = “Fair” (5% ≤ 20%)
Red = “Poor” (> 20%)
Notes: As of April 2016

## Slide 14: Benefits = f(Pretreatment Condition)
MAP-21 Cracking
Green = “Good” (< 5%)
Yellow = “Fair” (5% ≤ 20%)
Red = “Poor” (> 20%)
Notes: As of April 2016

## Slide 15: Benefits = f(Pretreatment Condition)
MAP-21 Cracking
Green = “Good” (< 5%)
Yellow = “Fair” (5% ≤ 20%)
Red = “Poor” (> 20%)
Notes: As of April 2016

## Slide 16: Benefits = f(Pretreatment Condition)
MAP-21 Cracking
Green = “Good” (< 5%)
Yellow = “Fair” (5% ≤ 20%)
Red = “Poor” (> 20%)
Notes: As of April 2016

## Slide 17: Benefits = f(Pretreatment Condition)
CCPR
CIR
No Rutting
No Cracking
Foam
Emulsion
Notes: As of April 2016

## Slide 18: Summary
Value of good materials, designs, construction, inspection
Life extendingx & condition improvingy preservation benefits
Measured reduction in subgrade moisture contents
Similar trends in south vs north, low vs high traffic sections
Planning underway for 2019 northern CR, FDR sections
Anticipate long term data collection for many years to come
Support for state agency decision process implementation
20 US state DOTs now supporting pooled fund, more likely.

## Slide 19
http://www.omnicrete.com.au/road-safety-surfacing/
High Friction Surface Treatments

## Slide 20
Dr. R. Buzz Powell, PE
Assistant Director
277 Technology Parkway
Auburn, AL 36830
Phone: (334) 844-6857
Cell: (334) 750-6293
Email: buzz@auburn.edu
Web: www.pavetrack.com
Twitter: www.twitter.com/pavetrack